| S.No | Inputs |  |  |  | Outcomes |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Laser Power PLZ | Scanning Speed SSP | Number of passes PC | Laser Frequency FLZ | Surface waviness SW | Material Vaporization rate MVR | Heat affected zone HAZ |
|  | W | (mm/min) | no unit | (kHz) | (µm) | (mm3/sec) | (µm) |
| 1 | 8.5 | 280 | 24 | 48 | 6.07 | 100.71 | 90.05 |
| 2 | 6.5 | 360 | 12 | 18 | 4.01 | 74.77 | 71.88 |
| 3 | 10.5 | 200 | 36 | 18 | 6.75 | 119.88 | 102.71 |
| 4 | 6.5 | 360 | 36 | 58 | 5.1 | 79.11 | 85.07 |
| 5 | 6.5 | 200 | 12 | 58 | 6.01 | 93.27 | 89.82 |
| 6 | 8.5 | 280 | 18 | 38 | 5.9 | 99.84 | 88.42 |
| 7 | 10.5 | 200 | 12 | 18 | 6.05 | 117.2 | 89.89 |
| 8 | 8.5 | 320 | 24 | 38 | 5.66 | 95.14 | 88.12 |
| 9 | 6.5 | 360 | 12 | 58 | 4.13 | 66.76 | 74.46 |
| 10 | 10.5 | 360 | 36 | 58 | 5.23 | 82.97 | 85.36 |
| 11 | 8.5 | 280 | 30 | 38 | 6.26 | 110.85 | 93.12 |
| 12 | 10.5 | 200 | 36 | 58 | 7.32 | 115.82 | 108.08 |
| 13 | 10.5 | 360 | 36 | 18 | 4.9 | 90.99 | 82.88 |
| 14 | 6.5 | 200 | 12 | 18 | 5.6 | 102.68 | 86.30 |
| 15 | 8.5 | 240 | 24 | 38 | 6.44 | 115.36 | 93.28 |
| 16 | 7.5 | 280 | 24 | 38 | 6.02 | 102.48 | 89.51 |
| 17 | 10.5 | 360 | 12 | 18 | 4.33 | 86.1 | 75.64 |
| 18 | 8.5 | 280 | 24 | 28 | 5.94 | 107.2 | 89.40 |
| 19 | 9.5 | 280 | 24 | 38 | 6.21 | 108.79 | 90.81 |
| 20 | 6.5 | 200 | 36 | 58 | 7.1 | 122.52 | 106.40 |
| 21 | 6.5 | 360 | 36 | 18 | 4.69 | 87.58 | 78.76 |
| 22 | 6.5 | 200 | 36 | 18 | 6.63 | 114.14 | 94.76 |
| 23 | 10.5 | 200 | 12 | 58 | 6.43 | 107 | 94.59 |
| 24 | 10.5 | 360 | 12 | 58 | 4.69 | 78.57 | 81.59 |

| Output | Ridge Hyper parameter | Ridge R² | RF Hyper parameter | RF R² | XGB Hyperparameter | XGB R² | NN Hyperparameter | NN R² |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| surface Waviness | {'alpha': 1, } | 0.918 | {n_estimators=100, max_depth=10} | 0.981 | {n_estimators=100, max_depth=5, learning_rate=0.05} | 0.999 | {'hidden_layer_sizes': architecture=(6,4,3), alpha=0.001, learning_rate=0.0} | 0.979 |
| MVR | {'alpha': 1, } | 0.866 | {'n_estimators':100, 'max_depth':10} | 0.970 | {'n_estimators':100, 'max_depth':5, 'learning_rate':0.05, 'subsample':0.8} | 0.997 | {'hidden_layer_sizes:' architecture=(8,5,4), alpha=0.001, learning_rate=0.01} | 0.887 |
| Heat Affected Zone | {'alpha': 1, } | 0.941 | {'n_estimators':100 ,'max_depth':10} | 0.974 | {'n_estimators':100, 'max_depth':5 ,'learning_rate':0.05, 'subsample':0.8} | 0.998 | {'hidden_layer_sizes': architecture=(6,4,2), alpha=0.001, learning_rate=0.01} | 0.744 |

Hyperparameter

Ensemble Performance Summary

| Ensemble Model Performance Summary |  |  |  |
| --- | --- | --- | --- |
| Target | RMSE | MAE | R² |
| Surface Waviness | 0.0668 | 0.0561 | 0.9944 |
| MVR | 1.3266 | 1.0954 | 0.9925 |
| Heat Affected Zone | 0.5858 | 0.5000 | 0.9956 |

SURFACE WAVINESS

MVR

HAZ

| Table 3: Optimal Laser Process Parameter |  |  |  |
| --- | --- | --- | --- |
| Parameter | Min SW | Min HAZ | Balanced |
| Laser Power | 6.50 | 6.50 | 6.50 |
| Scanning Speed | 360.00 | 360.00 | 360.00 |
| Number of passes | 12.00 | 12.00 | 12.00 |
| Laser Frequency | 18.00 | 18.00 | 18.00 |
| Surface Waviness | 4.045 | 4.045 | 4.045 |
| HAZ | 72.287 | 72.287 | 72.287 |

| Table 3: Optimal Laser Process Parameter |  |  |  |
| --- | --- | --- | --- |
| Parameter | Min HAZ | Max MVR | Balanced |
| Laser Power | 6.50 | 6.50 | 10.50 |
| Scanning Speed | 360.00 | 200.00 | 200.00 |
| Number of passes | 12.00 | 36.00 | 12.00 |
| Laser Frequency | 18.00 | 58.00 | 18.00 |
| Heat Affected Zone | 72.287 | 102.351 | 90..342 |
| MVR | 75.847 | 120.486 | 115.970 |

| Table 3: Optimal Laser Process Parameter |  |  |  |
| --- | --- | --- | --- |
| Parameter | Min SW | Max MVR | Balanced |
| Laser Power | 6.50 | 10.50 | 10.50 |
| Scanning Speed | 360.00 | 200.00 | 200.00 |
| Number of passes | 12.00 | 36.00 | 36.00 |
| Laser Frequency | 18.00 | 18.00 | 18.00 |
| Surface Waviness | 4.045 | 120.486 | 120.486 |
| MVR | 75.847 | 102.351 | 102.351 |